# SECTION 09 22 14

METAL FURRING AND LATHING

PART 1	GENERAL

- RELATED DOCUMENTS

  - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 specification sections, apply to work in this section.

- SECTION INCLUDES

  - Walls, bulkheads, and ceilings

  - Metal lathing for wet plaster finish

  - Section 08 31 00 – Access Doors and Frames

- SYSTEM DESCRIPTION

  - The extent of the use of metal furring and lathing as indicated on the drawings and/or specified.

  - Fabricate horizontal ceiling and soffit framing to limit finish surface to 1/240 deflection under superimposed dead loads and wind uplift.

- REFERENCES

  - ASTM C841 – Standard Specification for the Installation of Interior Lathing and Furring

  - ASTM C847 – Standard Specification for Metal Lath

  - ASTM C933 – Standard Specification for Welded Wire Lath

  - ASTM C1063 – Standard Specification for Installation of Lathing and Furring to Receive Interior and Exterior Portland Cement-Based Plaster

  - GA-600 – Fire Resistance Design Manual

  - EMLA (Expanded Metal Lath Association) – Guide Specifications for Metal Lathing and Furring

  - ASCE 7 – Minimum Design Loads of Buildings and Other Structures

  - Florida Building Code (FBC)

- SUBMITTALS

  - Shop Drawings: Indicate prefabricated work, component details, stud layout, framed openings, anchorage, type and location of fasteners, and accessories or items required of other related work.

  - Product Data:  Provide data describing standard framing member materials and finish, product criteria, load charts and limitations.

- DELIVERY, STORAGE, AND HANDLING

  - Deliver materials and store off the floor in dry area.

    - When moisture occurs, immediately remove water and allow members to completely dry.

  - Installation of rusted furring members is not acceptable.

PART 2	PRODUCTS

- FRAMING MATERIALS

  - Main Runner Channels; 1½" cold rolled, 16-ga steel, galvanized weight 500lb/1,000 LF.

  - Cross Furring Channels; ¾" cold rolled, 16-ga steel, galvanized weight 300lb/1,000 LF.

  - Hanger wire shall be 8-ga galvanized annealed.

  - Tie wire shall be 16-ga galvanized annealed for framing members.

  - Hangers: Galvanized steel, of size and type to suit application, rigidly support-ceiling components in place, and meet deflection limits as indicated.

  - Lateral Bracing:  Formed steel; minimum 16-ga thick; size and length as required.

  - Casing Bead, formed zinc minimum 26-ga thick; ground depth governed by plaster thickness; maximum possible lengths; expanded metal flanges, with square edges.

    - Product: ClarkDietrich; #66X Zinc Expanded Flange Casing Bead, or comparable product.

  - Corner Bead, formed zinc minimum 26-ga thick; depth governed by plaster thickness; maximum possible lengths; expanded metal flanges, with radii edge.

    - Product: ClarkDietrich; #1A Expanded Corner Bead, or comparable product.

  - Base Screed, formed zinc minimum 26-ga thick; ground depth governed by plaster thickness; maximum possible lengths; expanded metal flanges, with beveled edge.

    - Product: ClarkDietrich; Foundation Weep Screed , or comparable product with specified ground.

  - Control and Expansion Joint Accessories, formed zinc minimum 26-ga thick; accordion profile, 2" expanded metal flanges each side, with plaster ground thickness.

    - Product: ClarkDietrich; #15 Double-V Control Joint, or comparable product.

    - Product: ClarkDietrich; #40 Two-Piece Expansion Joint, or comparable product.

  - Install plaster frames for recessed light fixtures furnished by electrical contractor under this section.

  - The owner will consider vinyl beads and other accessories with documentation indicating the product performs equivalently with the metal system.

- LATHING MATERIALS

  - Metal Lath; ASTM C847; self-furring diamond mesh sheet; 3.4 lb/sq ft.

    - Product: ClarkDietrich; Self-Furring Dimple Lath , or comparable product.

  - Corner Mesh: Formed sheet steel; minimum 26-ga thick; expanded flanges shaped to permit complete embedding in plaster; minimum 4" size, as needed.

  - Strip Mesh:  Expanded metal lath, minimum 26-ga thick 4" wide x 24" long, as needed.

- ACCESSORIES

  - Tie wire, nails, screws and other supports, of type and size rigidly securing materials in place.

- FINISHES

  - Framing Materials: Galvanized

  - Hangers, Anchors and Fastening Devices: Galvanized

  - Lath Materials: G60 Galvanized

  - Lathing Accessories: Zinc Alloy

PART 3	EXECUTION

- EXAMINATION

  - Verify that conditions are ready to receive work.

  - Verify field measurements are as shown on drawings.

  - Beginning of installation means installer accepts existing conditions.

- CEILING AND SOFFIT FRAMING

  - Install furring to height indicated, erect after above ceiling or soffit work is complete.

    - Coordinate the location of hangers with other work.

  - Install furring independent of walls, columns and above ceiling work.

  - Securely anchor hangers to structural members or embed in structural slab.

    - Space hangers to achieve deflection limits indicated.

  - Space the main carrying channels at maximum of 72" centers, and not more than 6" from walls.

    - Lap the splices securely.

  - Securely fix carrying channels to hangers, prevent turning/twisting and transmit full load to hangers.

  - Place furring channels perpendicular to carrying channels, not more than 2" from perimeter walls, and rigidly secure.

    - Lap the splices securely.

  - Reinforce openings in suspension system that interrupt main carrying channels or furring channels with lateral channel bracing.

    - Extend bracing minimum 24" past each opening.

  - Laterally brace suspension system.

- CONTROL AND EXPANSION JOINTS

  - Install control and expansion joints as described in ASTM C1063.

    - Set both beads over 6" wide strip of rubberized-asphalt, peel and stick sheet to assist with air seal continuity.

  - Provide Control Joint Spacing as indicated on reflected ceiling plan, per ASTM C1063.

  - Provide Expansion Joint Spacing as indicated on reflected ceiling plan, per ASTM C1063.

- LATHING

  - Apply metal lath taut, with long dimension perpendicular to supports.

  - Lap ends minimum 1", and secure end laps with tie wire where they occur between supports.

  - Lap sides of diamond mesh lath minimum 1½", not to exceed 3 inches.

  - Attach metal lath to metal supports using tie wire at maximum 6" o. c.

  - Attach metal lath to concrete and concrete masonry using wirehair pins.

    - Securely attach the anchors to backup surface and spaced a maximum 24" o. c.

  - Continuously reinforce internal angles with corner mesh, except where the metal lath returns 3" from corner to form the angle reinforcement; fasten at perimeter edges only.

  - Place corner bead at external wall corners; fasten at outer edges of lath only.

  - Place base screeds at termination of plaster areas; secure rigidly in place.

  - Place 4" wide strips of metal lath centered over junctions of dissimilar backing materials.

    - Secure rigidly in place.

  - Place lath vertically above each top corner, each side of door, and glazed frame to 6" above ceiling.

  - Place casing beads at terminations of plaster finish.

    - Butt and align ends.

    - Secure rigidly in place.

  - Place strip mesh diagonally at corners of lathed openings.

    - Secure rigidly in place.

- TOLERANCES

  - Maximum Variation from True Position: ⅛" per 10'

  - Maximum Variation of any Member from Plane: ⅛"

END OF SECTION