SECTION 10 73 26

WALKWAY COVERINGS

PART 1	GENERAL

- RELATED DOCUMENTS

  - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division-1 specification section, apply to work of this section.

    - Section 31 20 00 – Earth Moving

    - Section 03 11 00 – Concrete Formwork

    - Section 03 30 00 – Cast-in-Place Concrete

- SECTION INCLUDES

  - Design, fabricate, and install a welded, extruded aluminum walkway cover with protective finish and illumination of covered areas.

- REFERENCES

  - AAMA 603.8 – Voluntary Performance Requirements & Test Procedures for Pigmented Or

  - AAMA 606.1 - Voluntary Guide Specifications and Inspection Methods for Integral Color Anodic Finishes for Architectural Aluminum

  - AAMA 607.1 – Voluntary Guide Specifications and Inspection Methods for Clear Anodic Finishes for Architectural Aluminum

  - AAMA 608.1 – Voluntary Guide Specifications and Inspection Methods for Electrolyically Deposited Color Anodic Finishes for Architectural Aluminum

  - AAMA 2603 – Voluntary Specification, Performance Requirements and Test Procedures for Pigmented Organic Coatings on Aluminum Extrusions and Panels

  - AAMA 2604 – Voluntary Specification, Performance Requirements and Test Procedures  for High Performance Organic Coatings on Aluminum Extrusions and Panels

  - ASCE 7- - Minimum Design Loads for Building and Other Structures

  - ASTM B206/B206M – Standard Specification for Copper Nickel Zinc (Nickel Silver) Wire and Copper Nickel Alloy Wire

  - ASTM B211- Standard Specification for Aluminum and Aluminum Alloy Rolled or Cold Finished Bar, Rod and Wire

  - ASTM B221- Standard Specification for Aluminum and Aluminum Alloy Extruded Bars, Rods, Wire, Profiles, and Tubes

  - FBC - Florida Building Code

- SUBMITTALS

  - Submit shop drawings including plans, elevations, and details, with dimensions and grades, for approval by Architect.

  - Submit manufacturer's product information, specifications, and installation instructions for review by Architect.

  - Submit design calculations signed by a State of Florida Professional Engineer verifying the walkway cover system design meets wind loading requirements of ASCE 7, live and dead loads, footings and other load requirements.

- DELIVERY, STORAGE, AND HANDLING

  - Deliver, store and protect products as instructed by manufacturer.

  - Promptly inspect shipment to assure the products comply with requirements, quantities are correct, and products are undamaged.

  - Stack the materials to prevent twisting, bending, or abrasion, and to provide ventilation.

    - Slope metal sheets to ensure drainage.

  - Prevent contact with materials during storage, which may cause discoloration or staining.

- QUALITY ASSURANCE

  - Manufacturer shall be a specialist with a minimum 5-years documented experience in manufacturing product.

  - Installer shall be specialized with a minimum 5-years documented experience in erecting, applying the work, approved, and certified by manufacturer.

- WARRANTY

  - Provide a 5-year warranty that shall include coverage for structural, water tightness and finish beginning the day of Substantial Completion.

PART 2	PRODUCTS

- DESIGN

  - Design loads for the structure and accessories, auxiliary and collateral loads shall comply with FBC and ASCE 7.

    - Use exposure category C, Risk Category III, for wind design.

    - Live load = 20 pounds per sq. ft.

  - Design the structure for temperature change of 100° F.

- COMPONENTS

  - Aluminum members shall be extruded aluminum alloy 6063, heat-treated to T-6 temper.

  - Columns shall be radius-cornered tubular extrusions with cutout and internal diverter for drainage.

  - Beams shall be open-top tubular extrusions; top edges thickened for strength and designed to receive deck members in a self-flashing manner.

    - Install extruded structural ties in the top of all beams.

  - Deck shall be extruded self-flashing sections interlocking into a composite unit with sufficient camber to offset dead load deflection and cause positive drainage.

    - Use welded plates as closures at deck ends.

  - Fascia shall be manufacturer's standard shape and a minimum 0.040 aluminum.

  - Fasteners shall be aluminum, 18-8 stainless steel, 300 series stainless steel, or 410-stainless steel with neoprene washers.

  - Protect aluminum columns embedded in concrete with clear acrylic.

  - Grout shall be 2,000-psi compressive strength; concrete 2,500-psi minimum.

  - Gaskets shall be dry seal pressure type of manufacturer's standard material.

- FABRICATION

  - Beams and columns shall be factory welded with mitered corners into one-piece rigid bents.

    - Welds shall be smooth and uniform using inert gas shielded arc, with 100% penetration.

    - Grind welds only where interfering with adjoining structure to allow a flush connection.

  - Field welding is not permitted, use rigid mechanical joints when shipping limitations exist.

  - Deck shall be extruded modules that interlock to form a self-flash condition.

    - Positively fasten interlocking joints at 8" on center forming a monolithic structural unit to develop the full strength of the sections.

    - Fastenings shall have minimum shear strength of 350 pounds each.

    - Assemble the deck with sufficient camber to offset dead load deflection.

- FACTORY FINISH

  - As selected by the Architect one of the following shall apply:

  - Factory-baked enamel - AAMA 603.8, standard or custom color, as selected.

  - Clear anodized - AA-M-10C-22A-31 (AAMA 607.1).

  - Bronze or black anodized - AA-M-10C-22A-44 (AAMA 606.1).

PART 3	EXECUTION

- EXAMINATION

  - Examine the areas and conditions where installing walkway covers.

  - Notify the contractor of any unsatisfactory conditions.

- ERECTION

  - Erect the walkway covers true to line, level and plumb.

    - Protect all aluminum columns in concrete with clear acrylic to prevent electrolytic reaction.

  - Downspout columns shall have welded water diverters or other material at the discharge level to prevent standing water.

    - Non-draining columns shall have weep-holes at concrete grade level to remove condensation.

    - Do not allow discharge to drain across walkways.

  - Provide concrete splash blocks in size and location to prevent washout of lawn or landscape.

    - Grade the adjacent area for water to drain away from walkways.

  - Devices, screws, bolts, and crimps shall be on topside of deck with none visible on the underside.

- CLEANING

  - Clean and polish the walkway component upon completion.

- PROTECTION

  - Take extra care to protect materials during and after installation.

  - Remove and replace damaged and defective members.

END OF SECTION