PART 1 - GENERAL

1.01	SUMMARY

A.	Provisions of Division 01 apply to this section.

B.	Section Includes:

1.	Prefabricated plywood web joists.

C.	Related Sections:

1.	Section 01 45 23: Testing and Inspecting Services.

2.	Section 06 10 00:  Rough Carpentry.

1.02	SUBMITTALS

A.	Shop Drawings: Submit Shop Drawings indicating joist locations, sizes, camber, spacing, species, stress grades and attachment details.

B.	Evaluation Reports: Submit research or evaluation reports stating 	compliance to CBC.

1.03	QUALITY ASSURANCE

- Comply with following as a minimum requirement:

  - ALSC – American Lumber Standards Committee: Softwood Lumber Standards.

  - APA – The Engineered Wood Association.

  - ICC – International Code Council Evaluations Service, Inc.

  - ASTM D2559 – Adhesives for Structural Laminated Wood Products for use under Exterior Exposure Conditions.

  - ASTM D5055 – Standard Specification for Establishing and Monitoring Capabilities of Pre-Fabricated Wood I-Joists.

  - National Bureau of Standards – Product Standard PS-1-95 for Construction and Industrial Plywood.

- Each member shall be stamped with an identifying mark.  Manufacturer shall provide a verified report identifying members by mark and including pertinent data such as certification of flange material and species, type of glue, and other information as may be required.

- Plywood web joist fabrication shall be inspected as part of manufacturer’s approved quality assurance program.  Inspection shall be performed in accordance with Section 01 45 23:  Testing and Inspecting Services.

1.04	DELIVERY, STORAGE AND HANDLING

A.	Store plywood web joists above grade on platforms, skids, or other required supports.

B.	Protect joists from moisture with polyethylene film or waterproof paper.

PART 2 - PRODUCTS

2.01	ACCEPTABLE MANUFACTURERS

- Standard Structures, Inc.

- Louisiana-Pacific Corporation.

- Georgia-Pacific Corporation.

- Boise Engineered Wood Products, BCI Joists, ICC/ES No. ESR-1336

- Red Built, Inc., Red-I Joist, ICC/ES No. 2994

- Weyerhauser, iLevel, TJI Series, ICC No. ESR-1153

2.02	MATERIALS

A.	Wood Chord: Solid-sawn lumber, laminated veneer lumber (LVL), laminated strand lumber (LSL) or machine-stress-rated (MSR) structural lumber.  Allowable unit stresses for chord members shall be as set forth in applicable NER or ICC reports.  Lumber grade identification shall be as indicated on Drawings.

B.	Web shall be plywood or oriented strand board.

C.	Accessories: Supply miscellaneous accessories including bracing, blocking, stiffeners, bearing clips, and any other required accessories required by joist manufacturer to complete joist installation.

D.	Adhesives: Adhesives must meet requirements for exterior type complying with ASTM D 2559.

2.03	FABRICATION

- Fabricate joists to achieve structural requirements specified.

- Verify dimensions and site conditions prior to fabrication.

- Fabricate joists in accordance with referenced standards.

PART 3 - EXECUTION

3.01	GENERAL

A.	Joists shall be of sizes and spacing indicated.  Top and bottom chord and web members shall be of sizes and stress-grade lumber indicated or specified.

3.02	INSTALLATION

- Verify that supports and openings are ready to receive joists.

- Verify sufficient end bearing area.

- Beginning of installation means acceptance of existing conditions.

- Coordinate placement of bearing items.

- Joints shall be installed in accordance with Drawings and Shop Drawings.

- Temporary construction loads, which cause stresses beyond design limits, shall not be applied to joists.

- Installation bracing, in addition to specified bridging, bracing shall be provided as required to keep joists straight and plumb until sheathing material has been installed.

- Fit members together accurately without trimming, cutting, or any other unauthorized modifications.

- Place headers and supports to frame openings required.

- Frame openings between joists with lumber in accordance with Section 06 10 00: Rough Carpentry.

- Coordinate placement of decking with work of this Sections.

# 3.03	CLEANUP

A.	Remove debris, rubbish, and waste material and legally dispose of off 	Project site.

# 3.04	PROTECTION

A.	Protect Work of this section until Substantial Completion.

3.05	TOLERANCE

A.	Framing members: ½ inch maximum from true position.

# END OF SECTION