- GENERAL

  - SECTION INCLUDES

    - Poured in place resilient playground surfacing.

    - Installation contractor to have a C61/D12 license and/or be certified by the manufacturer.

    - Related work.  Playground equipment sub-grade preparation.

    - Related Sections:

      - Section 32 12 16:  Asphaltic Concrete Paving.

      - Section 11 68 00:  Playground Equipment and Structures.

(Primary Centers and Elementary Schools)

      - Section 11 68 00.01:  Playfield Equipment.

(Middle and High Schools)

      - Section 32 13 14:  Portland Cement Concrete Paving.

  - REFERENCES

    - CBC 2019

    - ASTM F-1292, Current Edition, Impact Attenuation Test Certification.

    - ASTM E108 Fire Test.  Product shall exhibit a minimum result of a Class A Rating.

    - ASTM E303, Skid Resistant Test Data.

    - CPSC – Consumer Products Safety Commission, Handbook for Public Playground Safety, Current Edition.

  - SUBMITTALS

    - Manufacturer's Product Literature and Specification Data.

    - ASTM F1292 - Impact Attenuation Test Certification for the poured-in-place system to be installed in compliance with the Critical Fall height as determined by the Playground Equipment to be installed in conjunction with the poured-in-place surfacing system.

    - Color:  Selected from manufacturer's color chart.  Choice by Owner to be determined prior to installation.

    - Manufacturer's Installation Instructions and Procedures:  Indicate substrate requirements and installation methods.

  - WARRANTY

    - Statement of Warranty for a minimum two-year period, Full Warranty, labor and materials.  Detailed Warranty Claim requirements of the Owner and specific procedures to be followed by the manufacturer in terms of response and repair of warranty claims.

- PRODUCTS

  - MANUFACTURERS

    - SpectraPour by SpectraTurf, Corona, Ca.

    - Tot Turf by Robertson Industries, Inc.

    - Or equal as approved in accordance with Division 1, General Requirements for Substitutions.

  - MATERIALS

    - Description:  Dual durometer poured-in-place system with wearing layer upper membrane and an underlying impact attenuation cushion layer.  The finished surface shall be porous, and capable of being installed at varying thickness to comply with Critical Fall height requirements of playground equipment installed in conjunction with the surface.

    - Materials:  The surface shall be manufactured from EPDM and SBR rubber compounds mixed with a 100 percent MDI based Polyurethane Resin.  Polyurethane containing any TDI shall not be allowed due to environmental regulations.

    - Cushion Course shall be a mixture of 3/8" shredded and a 1-3mm SBR rubber particles of heterogeneous distribution (50/50 mixture)  bonded by a polyurethane binder applied to 100 percent of the rubber and installed to a designated thickness as required by the Consumer product Safety's Commission's Guidelines and ASTM F1292 Test Criteria.

    - Wearing Surface shall be a mixture of black or colored EPDM granules bonded by a polyurethane binder applied to 100 percent of the granules and applied to a thickness of 3/8 inch over the cushion layer.  Color choice and blend ratios to be of color selected by the Owner.

    - Finish Texture:  Pebble grain.

    - Geotextile Fabric: Geotextile membrane applied over compacted and graded sub-base.

- EXECUTION

  - EXAMINATION

    - Verify that substrate is graded, smooth and ready to receive work of this Section.

    - Verify gradients and elevations of substrate are correct.

    - Compact aggregate sub-grade to 95 percent.

    - Install minimum 4 inch aggregate sub-base, compacted.

  - INSTALLATION

    - Concrete Perimeter:  As indicated on drawings and in accordance with Section 03 30 53 Site Work Concrete.

      - Concrete Perimeter Curb: 6 inch wide x 8 inch deep, extending under surface min. 16 inches. Top of concrete curb to flush with finished surface.

      - Concealed Concrete Curb (overrun Poured-in-place): backfill with aggregate and install surfacing over geotextile fabric over compacted aggregate sub-base to produce a continuous play surface.

      - Slope to drain as indicated in drawings but no less than 1.5 percent.

    - Concrete and Asphalt Concrete Paving Substrate: Refer to Sections 03320 Site Work Concrete and Section 02740 Asphaltic Concrete Paving.

      - Install 2 inches minimum thickness concrete or asphaltic concrete over compacted sub-base.

      - Saw Cut Poured-in-place: cut keyway 1 inch wide, 1 inch deep into hard surface.  Form edge of cushion to taper edge starting 5 inches from keyway cut.

      - Slope to drain as indicated in drawings but no less than 1.5 percent.

    - Manufacturer shall have manufactured and installed playground poured-in-place surfacing systems to current ASTM F1292 Test Criteria for a minimum of 5 years.  The installation of the poured-in-place product shall be completed by Manufacturer Certified Contractors or by direct employees of the Manufacturer's Installation Division.  Manufacturer's detailed installation procedures shall be submitted to the Architect.

    - Make necessary adjustments to system to accommodate playground equipment uprights installed into grade.

    - Install level in Path of Travel with no change in elevation to each playground equipment area from surrounding hardscape.

END OF SECTION